## Slide 1
COMPOSITE SOLUTIONS

## Slide 2: COMPOSITE REPAIRS
A composite wrap is a permanent repair method suitable for non-leaking pipe defects.
  Composite repair systems are currently used to repair pitting, dents, gouges and external corrosion.
  Internal corrosion can not be arrested, therefore, a composite can not permanently repair defects associated with internal corrosion.
Serve as an alternative to traditional pipeline repair methods
  Cut outs/replacement
  Full encirclement steel split sleeves

## Slide 3: COMPOSITE REPAIRS
Advantages over traditional repair methods
  No hot work
  No pressure reduction/interruption in service
  Reduction in emissions
  Quicker
  Cheaper
  Safer
Disadvantages
  Not able to UT after being repaired
  Quality control done in the field
    Without proper application a composite will not work as engineered

## Slide 4: COMPOSITE REPAIR SYSTEM DEFINITION
The repair system is defined as the combination of the following elements for which qualification testing is completed.
substrate (pipe)
surface preparation
composite material (repair laminate)
filler material
adhesive
application method

## Slide 5: COMPOSITE SYSTEMS
Repairs are engineered using test data that combines specific manufacturing, surface and material preparation and installation techniques.
  Don’t deviate from the preparation or installation techniques.
  Don’t substitute repair materials

## Slide 6: PPE
Minimum requirements:
Disposable overalls; keep resin off clothes and skin
Rubber gloves; use thick ones
Safety boots
Safety glasses – use goggles when mixing or if people working overhead
Remove soiled PPE before entering clean areas

## Slide 7: COMPOSITE REGULATIONS
DOT
  CFR 192.713 & 195.585
    “Repaired by a method that Reliable engineering tests and analyses show that can permanently restore the serviceability of the pipe”
ASME
  PCC-2 (Post Construction Committee)
    16 Composite Testing Criteria
  B 31.4 & B 31.8
    Specifies composites can be used on ≤ 80% general corrosion pitting, and on some dents, gouges, wrinkles, etc. that are still piggable.
OQ Qualifications Needed for Training & Instillations
  Some training qualifications may be more extensive than others.
    Consider this when looking at the total cost of a system

## Slide 8: Choosing A Composite Repair System
Application Parameters
Pipeline features and the pipe defect characteristics will determine which system is right for you.
Many repair systems will require exact measurements to size EACH repair.

## Slide 9: APPLICATION PARAMETERS
% of Wall Loss:
  Custom repairs sized for your exact parameters
    Many allow you to neglect the remaining strength, in the pipe, when sizing a composite repair.
Defect Size:
  Must over lap a minimum of 2” on each side

## Slide 10: APPLICATION PARAMETERS
Pressure:
  This is rarely the limiting factor for composite repairs.
  Some systems may require a reduction in pressure for installation.
Temperature:
  Extreme temperatures require special resins
    Reduce repair lifespan

## Slide 11: APPLICATION PARAMETERS
Pipe Features:
  Is it a straight piece of pipe?
    If not, some systems are eliminated.
  A complete composite package, for a company, should be able to cover all pipeline features in their system.

## Slide 12: APPLICATION PARAMETERS
Repair Area Access:
  Room to work
  Pipe preparation
  Remote locations

## Slide 13: MEASURING STRENGHT
Nothing is specifically approved
  Must meet minimum requirements
Strength sets the systems apart
  Load Transfer
  Lap Sheer Strength
  Tensile Strength
      Testing information is always available

## Slide 14: Load Transfer
External defects are filled with a high compressive strength material
The hoop load is transferred though this material to the composite
The composite distributes the load throughout it’s layers around the pipe.

## Slide 15: Choosing A Composite Repair System
Composite System Strength
  Lap Shear Strength
    The strength demonstrated by the diagonal pull of two substrates until adhesive failure.
    The name comes from the lap joint created by the test samples and the shear action used to pull the samples apart.

## Slide 16: Choosing A Composite Repair System
Composite System Strength
  Tensile Strength
    Measures the force required to pull something to the point where it breaks.
    The tensile strength of a material is the maximum amount of tensile stress that it can take before failure, for example breaking.

## Slide 17: COMPOSITE REPAIR TYPES
Prefabricated
Wet Lay Ups
  Pre-Impregnated
  Field Wet Out
Machine Installations

## Slide 18: PREFAB COMPOSITES
Benefits
  Uniform Quality Control
  Less Messy
  Prepackaged Kits
    (one size fits all)
Disadvantages
  Only Straight Pipe
  Set Number of Wraps
  Not For Internal Corrosion

## Slide 19: PREFAB INSTALLATION
*General Installation Procedures – OQ Qualification Needed For Installation

## Slide 20: WET LAY UP COMPOSITES
Benefits
  Can Repair Irregular Pipe Features
  Higher Temperatures
  Engineered To Each Specific Application
Disadvantages
  QC Must Be Done In Field (In Most Cases)
  Messier
  Installation Time May Be Longer
  Not For Internal Corrosion

## Slide 23
This snapshot of our repair calculator shows how the input is used to calculate the repair. Note that we always use the long term strength of the composite so we can design external corrosion repairs to the lifetime of the host pipe.

## Slide 24: WET LAY UP INSTALLATION Field Impregnated

## Slide 25: WET LAY UP INSTALLATION Factory Pre-Impregnated

## Slide 26: MACHINE INSTALLATION
Benefits
  Long Runs Of Pipe
  30% Cheaper Than Replacing Pipe
Disadvantages
  Must Excavate The Pipe Completely
  Too Expensive For Small Runs (<50ft)

## Slide 27: OTHER COMPOSITE USES

## Slide 28: Our Capabilities
We Can Engineer The Job
Help Choose The Best System For Your Application
We Can Supply The Materials
We Can Train Installers
Provide Installation Oversight
Provide Composite Marking System For Smart Pig Detection