## Slide 1
Current Attenuation and ACVG Surveys
Gary Moss

## Slide 2
The PCM Performs Three Broad Functions
Locating Pipes and Cables
Current Attenuation Surveys
ACVG Surveys

## Slide 3
3
The PCM can….
Find contacts with other structures
Evaluate pipe coating for defects
Perform periodic pipeline surveys
Find defective insulation joints

## Slide 4: Pipe and Cable Locators Don't Find Pipes and Cables...
?

## Slide 5: ...They Find Electro-Magnetic Fields

## Slide 6: Why Does It Matter?
Because electro-magnetic fields do things that pipes and cables don’t do.
Buried conductors don’t move, but the fields they’re tracing are subject to…

## Slide 7
Which is Affected By:
Grounding
Peak or Null Antennas
Congestion
Frequency Applied
…Distortion

## Slide 8: Distortion - Grounding
Typical rectifier installation
Provides a perfect pipe connection point
Anode provides a perfect ground connection point
NACE Rocky Mountain Section Short Course 2015

## Slide 9: Distortion – Grounding: PCM+ Connection To Pipeline
Disconnect the rectifier output from both pipe and Anode
Connect the PCM transmitter in place of the rectifier
NACE Rocky Mountain Section Short Course 2015

## Slide 10: Distortion - Peak or Null Antennas
NACE Rocky Mountain Section Short Course 2015
1
2
3
Signal
response
1
2
3
Signal
response
Different aerial orientations can
be used for different responses
Peak
Null

## Slide 11: Distortion - Peak or Null Antennas
NACE Rocky Mountain Section Short Course 2015
In a clean electro-magnetic field, the peak and null antennas agree

## Slide 12: Distortion - Peak or Null Antennas
NACE Rocky Mountain Section Short Course 2015
In a distorted electro-magnetic field, the peak and null antennas do not agree, and the peak is always more accurate

## Slide 13: Distortion - Congestion
NACE Rocky Mountain Section Short Course 2015
Congestion creates a distorted field, which effects locate accuracy, depth estimation and current measurement.
Congestion can be created by a nearby line carrying the signal, a “T” in the line, a bend in the line or a change in the depth of the pipe.
Take your current and depth readings where peak and null agree and move several paces away from a bend or a “T” when taking your reading.

## Slide 14: Distortion – Frequency
To enable coating defects to be located the PCM+ uses very low frequency signal
4hz
Almost DC
Sticks to the pipeline
Less bleed off or coupling to other utilities
Increased distance (up to 19 Miles)
Why Do We Use 4Hz ?

## Slide 15: Benefits of Low Frequency

## Slide 16: Transmitter Settings – Output Frequency
ELF
Extra low frequency
4Hz & 98Hz / 128Hz
ELCD
Extra low frequency & current direction
4Hz, 8Hz & 98Hz / 128Hz
LFCD
Low frequency & current direction
4hz, 8hz & 512hz / 640hz
NACE Rocky Mountain Section Short Course 2015

## Slide 17: Transmitter Settings – Signal Output
Constant current output
100mA
300mA
600mA
1A
2A
3A
NACE Rocky Mountain Section Short Course 2015

## Slide 18: Taking Current Attenuation Measurements
NACE Rocky Mountain Section Short Course 2015
Use an independent ground and try to mimic your CP circuit when possible
Take your first measurement at least 150 feet from your connection point
Make sure rectifiers are not influencing the signal (turn off AND disconnect if necessary)
Isolate your circuit whenever possible (disconnect bonds for better surveys)

## Slide 19: Taking Current Attenuation Measurements
NACE Rocky Mountain Section Short Course 2015
Take readings at equal distances and record your distances
Every 50 feet is a good standard (others can be used dependent on location)
Use it as a macro tool and depth of cover tool (use A-frame for micro)
Look for anomalies with more than a 5% change normally
Make sure unit is upright and perpendicular to the pipe

## Slide 20: Taking Current Attenuation Measurements
NACE Rocky Mountain Section Short Course 2015
Stay on Peak and check peak and null readings and verify depth when readings are suspect
Take multiple readings in one location if you are suspect of the accuracy
Know what is in the area of your pipe and what it’s connected to
Use current direction to verify that signal is flowing back toward transmitter on pipe

## Slide 21: Practical Example
Chart: Distance

## Slide 22
Current Attenuation Graph
Actual PCM Results
3 steps are different looking in mA but nearly identical in dB

## Slide 23: Distribution of Current 1kHz vs. 4Hz

## Slide 24: Low Frequencies Go To The Short

## Slide 25: ACVG Is Used to Pinpoint Defect Location
Once survey is complete, use the A-Frame accessory to pinpoint defects
Connect the A-Frame to the locator
Set locator to ACVG
Must use either ELCD or LFCD
NACE Rocky Mountain Section Short Course 2015

## Slide 26: Transmitter Connections
NACE Rocky Mountain Section Short Course 2015
Rectifier
Test Station
Anodes
CP Rectifier
AC Feed
Pipeline
+
-
ACVG Tx

## Slide 27: ACVG - Pool of Potential
NACE Rocky Mountain Section Short Course 2015

## Slide 28: ACVG – Current Flow
NACE Rocky Mountain Section Short Course 2015
Current from the transmitter creates a voltage gradient around coating defects
Current density greatest at interface between the defect and the surrounding environment
Current density function of soil resistivity & Tx output
Transmitter

## Slide 29: ACVG – Using the A Frame
NACE Rocky Mountain Section Short Course 2015
Front of receiver
Directional Display
GREEN
RED
Keep the green pin facing forward

## Slide 30
Finding Coating Defects
NACE Rocky Mountain Section Short Course 2015

## Slide 31
ACVG – Receiver Readings
NACE Rocky Mountain Section Short Course 2015
44 dB
47 dB
50 dB
49 dB
46 dB
43 dB
An increase in voltage gradient will cause an increase in current density near a given coating defect on the pipeline under test
Signal current and voltage effects viewed on instrument’s display
Signal current direction is displayed as an arrow
Voltage is identified as decibels (dB)

## Slide 32
ACVG – Receiver Readings
NACE Rocky Mountain Section Short Course 2015

## Slide 33
ACVG – Receiver Readings
NACE Rocky Mountain Section Short Course 2015
Take 4 readings in a cross pattern - two in line with the pipe and two perpendicular to the pipe
All four arrows should point to the defect
Record highest dB reading

## Slide 34: Categorizing the Results*
0 – 30dB Ignore
30dB – 60dB Minor
60dB – 80dB Intermediate
80dB+ Major
NACE Rocky Mountain Section Short Course 2015
*Categories apply to normalized results @1A of 4Hz current. There is a formula for calculating the normalized results.

## Slide 35: Normalizing the Results
This gives you the number of dB to add or subtract from the reading, depending on whether the PCM (4Hz) current is above or below one Amp.
dB = 20*log(i/iref).
The iref is 1000 mA (one Amp). In the case of 500 mA the formula is 20 X log (500/1000), which equals +6 dB.
If the number is negative you add it and if it is positive you subtract it.
3.0A = +10dB relative to 1A
2.0A = +6dB relative to 1A
1.0A = 0dB relative to 1A
600mA = -4dB relative to 1A
300mA = -10dB relative to 1A
100mA = -20dB relative to 1A
31.6mA -30dB relative to 1A
10mA = -40dB relative to 1A
1mA = -60dB relative to 1A
NACE Rocky Mountain Section Short Course 2015

## Slide 36: ACVG Summary
NACE Rocky Mountain Section Short Course 2015
Use an independent ground and try to mimic your CP circuit when possible
Take readings parallel and along the pipe. When you see an arrow reversal go perpendicular to the pipe and make sure all four arrows point to the defect
You do not have to be right on top of the pipe when surveying
On concrete and asphalt use wet sponges or rags on the probes or wet the ground around the probes.
Take readings at equal distances usually about every ten feet
Use the largest dB reading seen around the anomaly for you records
Record all faults seen with dB readings and footages or GPS coordinates.
Take a PCM current reading at the site of the defect and adjust your dB reading to normalize for one Amp of current